COB932	CARACTERIZAÇÃO ÓPTICA E ESTRUTURAL DE FILMES DE KCl:Tl OBTIDOS POR EVAPORAÇÃO RESISTIVA

Elisabete Ap. A.Rubo(1,2), Máximo Siu Li(2) e Lígia de Oliveira(1)

1- Departamento de Física, FC-UNESP/Bauru,     CP 473 - CEP 17033-360 Bauru, SP - Brasil  - E-mail : rubo@ifqsc.sc.usp.br

2- Instituto de Física de São Carlos, USP/São Carlos,  CP 369 - CEP 13560-970, São Carlos, SP - Brasil

The study of defects in alkali halide thin films has shown new results about their optical and structural properties. In this work we present optical absorption results and structural characterization of  KCl:Tl+ films at 300K. The films were prepared by resistive evaporation and they are 0.5mm thickness. The absorption spectra show absorption bands at 250 and 197nm, like in crystals. If the impurity concentration increases in the film then the intensity of the optical absorption and its half width increases too. These films have 10+20 atoms/cm3 of Tl+ concentration and show a large absorption band; this feature suggest probable application for band pass filter.

Keywords: Alkali halides, KCl, thallium (Tl), thin films, resistive evaporation.