COB1059	MEDIDAS DE TAMANHOS DE GRÃOS AUSTENÍTICOS ORIGINAIS EM AÇOS TEMPERADOS / PRIOR AUSTENITIC GRAIN SIZE MEASUREMENT IN QUENCHED STEEL

Andrei Barban do Patrocínio, Luiz Carlos Casteletti

Departamento de Engenharia de Materiais, Escola de Engenharia de São Carlos- EESC/USP, Av. Dr. Carlos Botelho, 1465

CEP 13560-250 São Carlos, SP - Brasil - E-mail: Castelet@sc.usp.br

Special surface chemical treatments were performed on samples of hardened martensitic steel to show the original austenitic grains prior to quenching and tempering. Although the samples had a wide carbon content variation a high quality image of the austenitic grains was achieved, allowing computerized measurements. Considering all the formulas used, the compound with picric acid (6g), ether (100ml), water (100ml), hydrochloric acid (2ml) and neutral detergent (25ml) presented the best performance.

Keywords: Tamanhos de Grãos/Grains Size, Contornos de Grãos/Grain Boundary, Impacto/Impact, Ataques Metalográficos/Metallograpic Etching, Têmpera/Quenching.