COB264	CONSTRUÇÃO E ENSAIO DE UM CORPO NEGRO PARA OPERAÇÃO A BAIXAS POTÊNCIAS TÉRMICAS / CONSTRUCTION AND TESTING OF A BLACK BODY OF LOW THERMAL POWER

Alan C.B. Rocha, George S. Marinho, Leônidas Hildebrand Jr., Renê A. Carvalho*

* Instituto de Física de São Carlos. Departamento de Engenharia Mecânica, Escola de Engenharia de São Carlos - EESC / USP. Av. Dr. Carlos Botelho, 1465- São Carlos - SP - Brasil. CEP - 13560-250.

A cavity capable of working as a black body radiator was built and tested. Whereas most comercial systems work with the cavity body fixed to the core of a heated cylinder, the new device is directly heated by means of electric resistors fixed along its external surface. The electric resistors are heated by a highly stable dc-power system, which allows the cavity to reach temperatures of the order of 250oC. Constructed in a cone-type shape, the cavity has the back wall shaped with a large number of small pyramids, forming grooves. Its internal surface is roughly machined, forming a trap of baffles to radiation, wich leaves the cavity after multiple reflections through a unique small opening at the top of the cone. The main advantages of the system are its low cost and the simplicity of  assemblying. Emissivities as high as 0.96 were measured.

Keywords: Black body, thermal cavity, emissivity, pyrometer, thermal radiation. Corpo negro, cavidade térmica, emissividade, pirômetro, radiação térmica.