COB22	ASPECTOS FÍSICO-QUÍMICOS DA DECOMPOSIÇÃO SPINODAL m ® t OBSERVADA EM LIGA DE TITÂNIO BETA METAESTÁVEL/ PHYSICO-CHEMICAL ASPECTS OF THE SPINODAL DECOMPOSITION IN    A BETA TITANIUM    ALLOY

Ricardo Artur Sanguinetti Ferreira () & Elisabeth Gautier ()

() Departamento de Engenharia Mecânica da UFPE, Rua Acadêmico Hélio Ramos s/n - Cidade Universitária    50740-530 Recife - PE

e-mail : Sanguinetti@npd.ufpe.br

() Laboratoire de Science et Génie des Matériaux Métalliques - École des Mines de Nancy, Parc de Saurupt 54042, Nancy Cedex, France

A beta titanium alloy Ti-5.0Al-2.0Sn-4.0Zr-4.0Mo-2.0Cr-1.0Fe ( by weigth) was solution treated and followed by quenching. In the supersaturation condition this alloy was reheated at 0.5o C/s and 5.0o C/s in order to study the sequences of phase transformation on the anisothermal conditions. In the fisrt stages of heating, a little modification was observed on the morphology microstructures before the precipitation of intermediary phases. Different zones of the matrix present a darker contrast as a consequence of fluctuations in the chemical composition. Chemical microanalysis obtaineid by EDS in transmission electron microscopy revealed that those darker zones were weakened in Mo, Cr and Fe solute elements. Morphological analysis in electron microscopy    revealed no interface between rich and poor zones of matrix. Electron diffraction patterns taken from it showed scattered spots in the same lattice. The results indicate that solute separation, has no interface and identical lattice for different zones, thus we conclude that spinodal decomposition occurs really in beta titanium alloy at low temperatures.

Keywords: Spinodal decomposition; Decomposition in -Ti; Phase transformation in -Ti; Decomposição spinodal