COB812	ESTUDO DA CINÉTICA DE CRESCIMENTO E DA  ESTABILIZAÇÃO DE GRÃOS EM LIGAS DO SISTEMA CU-ZN-AL / THE STUDY OF THE KINETIC OF GROWTH TO STABILIZE THE GRAIN GROWTH IN THE CU-ZN-AL SYSTEM

Ricardo Artur Sanguinetti Ferreira (†), Paulo César Botelho de Andrade (††) Severino  L. Urtiga Filho(†) e Ney F. de Quadros(†)

(†) DEMEC - Departamento de Engenharia mecânica da Universidade Federal de Pernambuco - UFPE - Av Acadêmico Hélio Ramos s/n Cidade Universitária 50.741-530, Recife-PE. - E-mail : Sanguinetti@npd.ufpe.br

(††) ITEP- Instituto de Tecnologia do Estado de Pernambuco - Av. Prof. Luís Freire 700 Cidade Universitária 54.740-540, Recife-PE.

The study  of the microstruture evolution is of fundamental importance for Cu-Zn-Al shape memory alloy. The growth of grain degrades the shape memory effect by the displacement of temperatures where the transformations are observed. The degradation can be softened by the control of grain boundary migration or precipitation as a consequence of the diffusion process. The process control can be obtained by the increase the activation energy, which is produced by addition of the alloy elements. In this study  was used a Cu-Zn-Zn alloy without the addition of elements. Based on the area criterion of the ASTM standard, the statistic measurements of a grain size were made in samples treated at different temperature of the ageing or annealing treatments. The kinetic of the grain growth was studied by an Arrhenius empirical law and the activation energy for this process (EA) was estimated by ln (D) x 1/T diagram. At lower temperatures, results of the activation energy follow either theoretical or experimental results. Moroever, for higher temperatures of the thermal treatments a change in the slope of the ln (D) x 1/T diagram was observed. This anomalous behavior was associated with a secondary recrystallization as a consequence of the intermediary thermomechanical treatments. On the morphological view point, the secondary recrystallization was characterized to produce an anormal grain size with many boundary faces. Important conclusions about grain growth mechanisms were obtained. After these results, a selection of some of the elements will be made to increase the activation energy (EA) in order to stabilize the grain size.

Keywords: Grain growth ; Kinetic of growth ; Activation energy ; Secondary Recrystallization. Cinética de crescimento