COB1020	ESTUDO DA DENSIFICAÇÃO DO AÇO INOXIDÁVEL 316L SINTERIZADO EM REATOR DE PLASMA / DENSIFICATION STUDIES OF 316L STAINLESS STEEL SINTERED IN A PLASMA REACTOR

Vilson João Batista, Jorge Hebert Echude Silva, Márcio Mafra, Joel Louis Rene Muzart, Aloísio Nelmo Klein

LABMAT - Pós Graduação em Engenharia Mecânica - UFSC,CEP. 88040-900, Florianópolis, SC, (vilson@labmat.ufsc.br), (echude@matrix.com.br), (mafra@labmat.ufsc.br), (joel@labmat.ufsc.br), (klein@labmat.ufsc.br).

This study shows the consolidation behavior of AISI-316L Stainless Steel sintered in a plasma reactor. Three thermal cycles were followed varying the sintering temperature and time.The final densities obtained here for the 316L- SS sintered by this novel technique were equal or higher than the densities of known steels sintered by conventional routes. Nevertheless, plasma sintering allows a better atmosphere control, as well as energy saving, since only the sintering parts are heated up by the ionized plasma. The main results include densities of the order of 7.39; 7.43 and 7.64 g/cm3 for sintering conditions of 1050 °C and 1150 °C during 60 min., and 1270 °C during 150 min.

Keywords: Plasma; Sinterização, Processo / Plasma; Sintering; Process.