COB567	RESISTÊNCIA AO CISALHAMENTO DE UNIÕES AÇO ZINCADO / EPÓXI / AÇO FOSFATIZADO / SHEAR STRENGTH OF ZINCATED STEEL / EPOXY ADHESIVE / PHOSPHATIZED STEEL JOINTS

Astrid Damasco1, Itamar Ferreira2, Marcelo C. Gandur3, Pedro A. P. Nascente1 e Nelson G. Alcântara1

1 Centro de Caracterização e Desenvolvimento de Materiais, Departamento de Engenharia de Materiais, Universidade Federal de

São Carlos, CEP 13565-905 São Carlos, SP, Brasil. ccdm@power.ufscar.br.

2 Departamento de Materiais, Faculdade de Engenharia Mecânica, Universidade Estadual de Campinas, CEP 13083-970

Campinas, SP, Brasil.

3 Divisão de Adesivos e Químicos, 3M do Brasil Ltda, Caixa Postal 123, CEP 13001-970 Sumaré, SP, Brasil.

The effects of sheet thickness (1.5 and 2.0 mm), cleaning state of the surface of the steel sheets (in a condition without cleaning and by using Metal Ethyl Ketone as a cleaner), and test time after bonding (24 and 96 hours) on the shear strength of galvanized steel / epoxy adhesive / phosphatized steel joints hava been analyzed. The results showed that the sheet thickness and the cleaning state of the steel sheets had no effect the shear strength; for these conditions the shear strength was about 9.7 MPa. On the other hand, the test time after bonding had a significant effect on the shear strength; the shear strength for the 24 h test time after bonding was 9.4 MPa and 10.4 MPa for 96 h. In all cases the standard deviation was very low: maximum of  5%.

Keywords: Metal/adhesive joints, Shear strength, Steel, Epoxy.