COB1268	DESARROLLO DE UN HIERRO NODULAR BAINÍTICO PARA FABRICAR PIEZAS DE EQUIPOS DE LA CONSTRUCCIÓN./ BAINITIC DUCTILE IRON FOR CONSTRUCTION MACHINES PARTS

Urbano Ordoñez, Efraín Pantaleón, Yvan Houbaert, Leonardo Goyos, & Carlos Diez

Departamento de Tecnología de Construcción de Maquinaria, Facultad de Ingeniería Mecánica,ISPJAE,

Habana, Cuba, Profesor Visitante en EPUSP, Depto de Engenharia Mecânica,Patrocinado por FAPESP. Email: urbyordz@usp.br

The aim of this work is the development of a fabrication technology for 1,0% copper alloyed bainitic ductile iron. The alloy is intended for using it in automotive, construction, agriculture and other related industries, where low alloyed carbon steel spare parts are imported at very high prices in hard currency. The principal task to be carried out was the selection of an optimum heat treating technology; that means; austenization and austempering parameters. Metallurgical quality of the alloy after the heat treatment was assessed by means of different tests including mechanical properties, optical and SEM microscopy and X rays diffraction and microanalysis. Strain hardening of the alloy was evaluated through a compression test. Austenization at 880 o C during two hours and austempering at 380 o C also during two hours were the selected parameters for heat treating of several spur gears and pneumatic hammers handles that are now being evaluated.

Keywords: hierro nodular bainítico, fabricación, tratamiento térmico / bainitic ductile iron, fabrication, heat treatment